CARUS( 3090 water treatment chemical is an effective corrosion inhibitor developed specifically for use in potable and industrial water systems.  The product is a liquid concentrate of exceptional purity, clarity, and stability.

- Forms a stable, highly resistant film on the inside of distribution piping and metal surfaces, providing for effective corrosion control.

- Inhibits corrosion of steel distribution system water lines, iron and galvanized piping, and lead and copper plumbing.

- Decreases iron tuberculation, which can extend the life of the distribution system.

- Lowers lead and copper levels in the delivered potable water by inhibiting corrosion in the water system.

- Decreases the potential for trihalomethane (THM) formation by using the product at a lower water pH.

- Protects against the release of asbestos or cement from water mains.

- Saves money by reducing corrosion, and decreasing hydrant flushing, leaks, and failures.

- Clear liquid

- Do not freeze.

- Best if used within one year

- NSF Maximum Feed Rate: 20 mg/L

- Specific Gravity: 1.31-1.37

- Conforms to ANSI/NSF Standard 60

- pH: <1.0

- Weight: 10.9-11.5 lbs. per gallon

CARUS( 3090 water treatment chemical is packaged and shipped in 55-gallon containers and is also available in bulk quantities.  The product is shipped in polyethylene drums or certified tankers.  Each container is identified by a lot number.  Avoid contact with eyes, skin, and clothing.  For complete information, please refer to the Material Safety Data Sheet (MSDS).

CARUS( 3090 water treatment chemical is applied using a chemical metering pump.  In most applications, the product is fed as a concentrate without the necessity of dilution.  For dosage rates or answers to technical questions, please call Carus Phosphates, Inc. at (800) 929-6789.

# Text boxes

PROPERTIES AND CERTIFICATIONS

(CARUS and Design) is a registered service mark of Carus Corporation.

# CARUS™ is a trademark of Carus Corporation.

Responsible Care( is a registered service mark of the American Chemistry Council.

BENEFITS OF CARUS™ 3090 WATER TREATMENT CHEMICAL

##### CARUS  PHOSPHATES INC.

181 Woodlawn Ave  (  Belmont, NC 28012

Tel: (704) 822-1441   Fax: (704) 822-0922

E-Mail: salesmkt@caruscorporation.com

Web: www.caruscorporation.com

Copyright 2007

Form #PH

Rev. 10/07

The information contained herein is accurate to the best of our knowledge. However, data, safety standards and government regulations are subject to change; and the conditions of handling, use or misuse of the product are beyond our control. Carus Corporation makes no warranty, either express or implied, including any warranties of merchantability and fitness for a particular purpose. Carus also disclaims all liability for reliance on the completeness or confirming accuracy of any information included herein. Users should satisfy themselves that they are aware of all current data relevant to their particular uses.

CARUS™ 3090

Water Treatment Chemical

SHIPPING AND HANDLING

APPLICATION