CARUS( 3290 water treatment chemical is an effective corrosion inhibitor developed specifically for use in potable and industrial water systems.  The product is a liquid concentrate of exceptional purity, clarity, and stability.

- Forms a stable, highly resistant film on the inside of distribution piping and metal surfaces, providing for effective corrosion control.

- Inhibits corrosion of steel distribution system water lines, iron and galvanized piping, and lead and copper plumbing.

- Decreases iron tuberculation, which can extend the life of the distribution system.

- Lowers lead and copper levels in the delivered potable water by inhibiting corrosion in the water system.

- Minimizes the occurrence of microbial-induced corrosion, providing longer system life.

- Reduces discoloration, staining, and sediment buildup in the water system, resulting in fewer customer complaints.

- Decreases the potential for trihalomethane (THM) formation by using the product at a lower water pH.

- Protects against the release of asbestos or cement from water mains.

- Saves money by reducing corrosion, lowering chlorine demand, and decreasing hydrant flushing, leaks, and failures.

- Clear liquid

- Best if used within one year

- NSF Maximum Feed Rate: 25 mg/L

- Specific Gravity: 1.37-1.43

- pH: < 1.0

- Weight: 11.6-12.1 lbs. per gallon

- Conforms to ANSI/NSF Standard 60

CARUS( 3290 water treatment chemical is packaged and shipped in 30- and 55-gallon containers and is also available in bulk quantities.  The product is shipped in polyethylene drums.  Each container is identified by a lot number.  Avoid contact with eyes, skin, and clothing.  For complete information, please refer to the Material Safety Data Sheet (MSDS).

CARUS( 3290 water treatment chemical is applied using a chemical metering pump.  In most applications, the product is fed as a concentrate without the necessity of dilution.  For dosage rates or answers to technical questions, please call Carus Phosphates, Inc. at (800) 929-6789.

# Text boxes

(CARUS and Design) is a registered service mark of Carus Corporation.

# CARUS™ is a trademark of Carus Corporation.

Responsible Care( is a registered service mark of the American Chemistry Council.

The information contained herein is accurate to the best of our knowledge. However, data, safety standards and government regulations are subject to change; and the conditions of handling, use or misuse of the product are beyond our control. Carus Corporation makes no warranty, either express or implied, including any warranties of merchantability and fitness for a particular purpose. Carus also disclaims all liability for reliance on the completeness or confirming accuracy of any information included herein. Users should satisfy themselves that they are aware of all current data relevant to their particular uses.

BENEFITS OF CARUS™ 3290 WATER TREATMENT CHEMICAL

CARUS™ 3290

Water Treatment Chemical

SHIPPING AND HANDLING

##### CARUS  PHOSPHATES INC.

181 Woodlawn Ave  (  Belmont, NC 28012

Tel: (704) 822-1441   Fax: (704) 822-0922

E-Mail: salesmkt@caruscorporation.com

Web: www.caruscorporation.com

Copyright 2007

Form #PH

Rev. 10/07

PROPERTIES AND CERTIFICATIONS

APPLICATION